The Shapes of Transients of SS316 in 3.5 % NaCl

The SS316 transient exhibit different shapes compared to SS304 in 3.5 % NaCl. Althought there were common transeints shapes but worth demonestrating the different shapes with different times.

Graph (6.14) exhibit the SS304 in 3.5% NaCl with the transients 12.7 µA with stability factor 0.16 A m-1 which indicate in not open pit. The cover here had last 1000 second with further indication that the pit is combination of two pit within each other. Once the cover of the first pit fall the second one had lasted enough time with strength.

With 100 mV potential drop the cover didn't fall completely and switched itself off by the mentioned potential drop. The long  survival duration of pit cover  suggest that the pit were perforated or lacy cover were dominating on the top of the pit mouth. The general outlook of transient suggest that the pit behaviour indicative of open pit and proportional to pit radius.

Then in graph (6.15) the pit current switched by potential with its classical shape of diffusion inclination current and once the cover fall the pit repassivate swiftly.

Graph 6.16 suggest that the same event repeated itself in both instances. The sign of the current suggest the opposite Working electrode had influenced by the pit. The transient here is metastable with stability factor less than 0.3 A m-1. It seems here that the chromium and Molybdenum were controlling the behaviour of the metal.

The graph (6.17) is a hybrid mixture of previous transients with strange shape of potential behaviour over a period of 10 seconds the potential drop recorded here  5   mV and the current  drop amplitude of  8 A.

This transient  with its finite time repassivation subjecate that the data acquisition system employed in this work was not adequate to make full investaigation of current and potential drop and required to be higher rate to deal with the behaviour of such transient.

The slow rise in potential accepted to be due to one of the following reasons or might be combination of them

1.

Double layer capacitor were functioning in this pit.

2.	Charge transfer resistance for oxygen reduction is very high.

3.	Corrsion potential for non pitting event were due to non zero current.

Evaluating the potential drop from 183 mV to 178 mV (i.e 5 mV difference) with the general shape of the current transient which is linear current (I proportional to time)  suggest that the driving force for the event was not able to polarize one of the working electrode.

The following graph 6.18  suggest that three metastable pits were surviving on the SS316 in seawater. This is possible although the time for sampling were betweeen 6500 to 6600 seconds. Different current amplitude  ranging  at levels (I) 35 , (II) 25 and (III) 34 nano Amps. Those small amplitude indicate some metastable pits were a live with typical duration of  10-25 seconds.

6.1.2 The SS316 immersed in Seawater and Brine

The graph ( 6.19) suggest that the seawater can influence the events in the same manner of 3.5% NaCl . The graph  suggest further transient which at time from 1 to 100 second  and 615 seconds two different transient had developed suggesting that the first transient follow the behaviour of classical stainless steel where the second transient behave like mild steel in passive solution.

The limitation of the data recording system in this work is the . The measurement resolution of the current is at a region of 1nA  and the transients level had been recorded almost within the mean round of the resolution suggested not to be recorded lower in the experimental work.

Graph(6.26) for stainless steel 316 immersed in brine share some common feature  with the graph(6.10) for stainless steel 304 immersed in seawater. The current is stable when does it culminated to the maximum for some time.

In Summary

Three different intrensic questions

1.	What is the difference between transients in NaCl and Seawater and Brine

2.	Is other events comming up in controlling the behaviour of transients other than diffusion.

3.	Does those transients suggest the cover failure on stages or the cover will fail at once?

Mechanism of Metastable Pit

The experimental results obtained in this work confirm that metastable pits can occur in stainless steel far below the potential required for stable pitting.  These metastable pits are appearing all the time in our experimental work, showing hemispherical shapes and covered by a layer of sodium chloride salt layer due to its supersaturation and then precipitation on the pit mouth.  This observation is not new to the field as many workers have reported this.[150]

At a temperature of 49oC, the stable pits appeared on stainless steel Avesta 904.  Focusing on stainless steels 304 and 316, the wire which is a commercial product of such alloys shows metastable pits on the surface immediately after immersion in 3.5% Nacl.  the lack of Molybdenum in the commercial types of stainless steel and by the presence of silica (Si), the initiation of pit occurred.  The inclusion of Mn-S which is thermodynamically unstable and could dissolute leaving space to migrated chloride enhances the metastable pit.  The polishing procedure of the stainless steel wire 304 would contribute to the surface roughness which is considered to be a further factor for the metastable pits birth.

The solution chemistry inside the pit can be studied by demonstrating the following reaction:

(i)	Anodic dissolution reactions

Fe		Fe++		+	2e-

Mo		Mo+++	+	3e-

Ni		Ni++		+	2e-

Cr		Cr+++		+	3e-

(ii)	The hydrolysis process with the presence of water

Fe++	+	H2O		(FeOH)+	+ H+

Ni++	+	H2O		(NiOH)+	+ H+

Mo++	+	H2O		(MoOH)++	+ H+

Cr+++	+	H2O		(CrOH)++	+ H+